## Slide 1
Numerical investigation of two-dimensional Mode-II delamination in composite laminates
Congzhe Wang, Anastasios P. Vassilopoulos, Thomas Keller
Ecole Polytechnique Fédérale de Lausanne

## Slide 2
Mode I: DCB
Mode II: ELS
Standardized tests
Limited information
Certain areas of application

## Slide 3
The ALOHA Airlines flight 243 (1988)

## Slide 4
The ALOHA Airlines flight 243 (1988)
https://www.youtube.com/watch?v=YYa7Fq5Ec6c

## Slide 5: Engineering for a sustainable future
Application areas

## Slide 6
Composite constructions in Europe

## Slide 7: Delamination in composites – 1D/2D/3D

## Slide 8
Crack front is (almost) never straight (?)

## Slide 9
Mode I (opening)
Mode II (sliding shear)
Mode III (tearing shear)
One-dimensional (1D) crack propagation
Constant crack width (beam width)
Free boundary at cracked ends
ISO 15024:2001 – Double cantilever beam (DCB) test
ISO 15114:2014 – End-loaded split (ELS) test
Delamination
Delamination in real structures
Decomposition
Two-dimensional (2D) crack propagation
P
P
P
?
Traditional fracture analysis?

## Slide 10
In the past… panels with central hole

## Slide 11
In the past…buckling/growth in stiffened panels

## Slide 12
In the past…Mode I 2D opening
Modeling of G: Theoretical formulation neglecting geometrical non-linearities
G (2D) was estimated to be ~33% lower than that estimated from DCB (1D) tests

## Slide 13
Wide single lap shear joints (WSLS)
Aircraft fuselage longitudinal joint
Low velocity impacted CFRP WSLS joint
Modelling the joint in Abaqus®
Work with ZHAW and Airbus, Germany.
Wide single lap shear joints (WSLS): Element level testing of aircraft fuselage joints/ repairs
CFRP adhesive joints: Impacted, water and ice, under fatigue loading.

## Slide 14: Previously – 2D Mode-I experiments
2D Mode-I experiment
P
P
P
1D (DCB)
P
P
2D
Membrane forces
Schematic illustrations of 1D and 2D Mode-I delamination experiments
Delamination growth

## Slide 15: Two-dimensional Mode-I delamination
Experimental investigation of 2D Mode-I delamination
Numerical investigation of 2D Mode-I delamination
vs
(a) DCB (Gtot=2.0 kJ/m2) (b) 2D (Gtot=2.8 kJ/m2)
Numerical model using cohesive elements with fiber bridging effects considered
Parametric study on 2D Mode-I delamination
Effects of:
Pre-crack size
Pre-crack shape
Loading-zone size
Loading-zone shape
Fracture toughness
Stiffness
Example of impact damage on Airbus A330 after horizontal stabilizer accident
Fracture in composites in real scenarios is usually two-dimensional (2D)
… …
Background

## Slide 16
2D Mode I delamination – additional validation

## Slide 17: 2D Mode-I experiments: What we learned?
P
P
1D (DCB)
P
P
2D
Membrane forces
Main differences from 1D tests
Increasing crack-front length
Constrained boundary at the crack wake
Appearance of membrane stresses
Resulting 2D effects
Increasing loads even after crack propagation
Enhancement of fiber bridging
Greater G
Schematic illustrations of 1D and 2D Mode-I delamination experiments

## Slide 18
2D Mode II delamination – experimental

## Slide 19
2D Mode II delamination – experimental

## Slide 20
2D Mode II delamination – 1D experiment
Material description

## Slide 21
2D Mode II delamination – experimental
Experimental results (a) 1D ELS, (b) 2D plate testing

## Slide 22
2D Mode II delamination – numerical modeling

## Slide 23
2D Mode II delamination – 1D numerical modeling
GII vs crack sliding at the insert tip and the derivative curves
Crack sliding at the insert tip in 1D (ELS) experiments
A semi-experimental method was developed to derive the softening traction-separation law based on video extensometer measurements.
Differentiation

## Slide 24
2D Mode II delamination – 2D numerical modeling
Schematic cohesive model
Independent variables: {Gtip, GIIc, K0, σc, σm, δ2, δf}
Iterative fitting for Models 1, 2a and 2b
1D
2D
Gtot=Gtip+Gm+Gbr
A new cohesive model was developed based on the
experimental estimation of the softening law.
The model considers the three major mechanisms observed in the FPZ during the experiments:

## Slide 25
2D Mode II delamination – 2D numerical modeling
Gtot=Gtip+Gm+Gbr
Segment O-A-B-C represents the matrix plastic damage ahead of the macro-crack tip.
Segment O-A corresponds to the material continuity
before damage onset, where σ increases linearly with δ at a high slope, i.e., penalty stiffness, K0.
After reaching the Mode-II interfacial strength, σc, at a separation of δc, the curve enters a plateau.
The traction drops abruptly at point B with a slope of -K0, indicating a rapid traction jump.

## Slide 26
2D Mode II delamination – 2D numerical modeling
Gtot=Gtip+Gm+Gbr
Segment C-D represents the microcracking-dominant mechanism, where the separation increases from δ1 to δ2 with a constant traction, σm. This corresponds to the plateau in the experimental softening law, reflecting the mean shear traction over multiple microcracks.
Segment D-E represents the fiber (bundle) bridging-dominant mechanism, which appears after the coalescence of the microcracks at the wake of the microcracking zone.
Segment D-E is described using the relationship at the right, which has been proven effective in modeling the bridging behavior in both 1D and 2D Mode-I delamination:

## Slide 27
2D Mode II delamination – 1D numerical modeling
Detailed cohesive laws
Modeling results – Both 1D and 2D

## Slide 28
2D Mode II delamination – membrane stresses
Deformed section of the 2D model
U: upper sub-laminate;
L: lower sub-laminate.
Radial membrane stresses along r axis (a=100 mm)
Model 2a: a0=40 mm;
Model 2a: a0=80 mm.
Stretching over the microcracking zone introducing extra opening component onto the microcracks
Similar membrane stress levels for Models 2a and 2b (stabilized values during crack propagation)

## Slide 29
2D Mode II delamination – numerical analysis
A new Mode-II cohesive law considering microcracking and fiber bridging was developed using a semi-experimental approach.
The analysis resulted in two distinct cohesive laws, one for the 1D case and another for the 2D cases.
The assumption of equal Gtip in 1D and 2D Mode-I and Mode II delamination was validated by comparisons between the numerical and experimental results regarding the crack initiation displacement (deflection).
GIIc value was similar for 1D and 2D regardless of the difference in the traction-separation response. This contradicts the results in Mode-I (1D, 2D) delamination and raises more questions for future investigations.

## Slide 30
2D Mode II delamination - publications

## Slide 31: Acknowledgments
“Fatigue and fracture simulation methods for engineering structures made of polymeric composites” (200020_185005)